## Slide 2
Weld Sensors for Robotic Welding
Intermediate Training
Jack Moore May 2018

## Slide 3
Theory: sensing technologies
  Seam finding
Seam Finding
  AccuFast setup
  Macro Job settings
  Applications
Seam Tracking
  Comarc tuning
Overview

## Slide 4
Touch Sensing
AccuFast
MotoSight 2D
Motoeye SF w/ Servo-Robot iCube
SeamTracking
Com-Arc (thru-the-arc)
MotoEye LT w/ Servo-Robot tracking Cameras
Adaptive Welding
Multi-Layer Welding
SeamFinding

## Slide 5
Sensor comparison
Touch Sensing
  Pro’s
    Low cost
    Reliable (most surfaces / metals)
    Easy to program
    Can be used with Toolsight
  Con’s
    Wire brake sometimes required (increased cost)
    Slower measurement time with thin electrodes / softer metals
    Wire clipping usually required (increased cycle time, increased programming complexity)
Usage
AccuFast
  Pro’s
    No wire clipping (simpler program logic, reduced cycle time)
    Easy to program
    Faster search speeds (especially for easy-to-bend electrodes) and faster search patterns
    Thinner materials / butt joints
    Can be used with the AccuFast Target
  Con’s
    Not applicable for highly reflective materials (shiny stainless steel, etc.)

## Slide 6
Theory – Seam Finding

## Slide 7
Overview
seam finding fundamentals

## Slide 8
Theory – Seam Finding

## Slide 9
Laser Spot Sensor
  Detects if the surface is “in range” based on a stand-off distance (which can be customized)
  If surface is “in range” / at the stand-off distance, or closer…
    “Wire touched” signal is sent to controller
    Robot briefly stops its motion
    Robot collects positional data
    Rob continues with macro job routine
Principles

## Slide 10
Keyence Sensor adjustments
Keyence sensor:
  General Navigation
  Display
  Settings for AccuFast
    LOW
    HIGH
    Averaging Filter
AccuFast - Setup
RIN#(x)=OFF
HI
LO
RIN#(x)=ON

## Slide 11
Keyence Sensor: Display
  During normal operation…
  Main display = used to show the current measured distance
  Secondary display (lower display) = shows the value of the parameter currently be adjusted
  The SELECT buttons are used to navigate to the various parameters (using left/right) and also to adjust the value of the given parameter (using up/down)
AccuFast - Setup

## Slide 12
Keyence Sensor adjustments: LOW
  The LOW setting is an application-critical setting. If you adjust this after you have programmed robot positions inside the Touch Macro Jobs, you will need to reprogram the robot positions of the Touch Macro Jobs and, thus, possibly weld path as well! Adjust this before you begin robot programming.
  Press LEFT/RIGHT select buttons until the LED labeled LO is lit.
  Press UP/DOWN to adjust for your application.
AccuFast - Setup
RIN#(x)=OFF
HI
LO
RIN#(x)=ON

## Slide 13
Keyence Sensor adjustments: HIGH
  The HIGH setting, for most settings, is a not an application-critical setting. Typically this HIGH value is set far from the LOW value. For most applications, bigger is better.
  Press LEFT/RIGHT select buttons until the LED labeled HI is lit.
  Press UP/DOWN to adjust for your application.
AccuFast - Setup
RIN#(x)=OFF
HI
LO
RIN#(x)=ON

## Slide 14
Keyence Sensor adjustments: Averaging Filter
  The AvE setting is an application-critical setting. Set this before starting robot programming. If adjusted after robot programming began, the robot positions of the Touch Macro job (and weld path) may need to be reprogrammed. 16 is default value.
  Press MODE
  Press SELECT Right or MODE until “3. AvE” is displayed
  Press UP/DOWN to adjust for your application.
    More reflective surface … larger number (ie. 32 or 64)
    Thinner lap joint / smaller “Lap Offset” (R*-TCH) / smaller “Depth” (R*-EDGE) … smaller number (ie. 16)
AccuFast - Setup

## Slide 15
OVERVIEW
Utilizes Macro Jobs
  Location of Reference Positions
    (covered in available videos)
  Settings to adjust search path(s)
    (covered in this class)
Macro Job interface
3 types of search routines
  TCH (“touch”):
    1D mode … for flat surfaces or edges
    2D mode … for fillet or lap joints
  EDGE: 6 modes
  CIRCLE
Robot Programming

## Slide 16
Seam Finding
1 search – edge of plates
  EDGE using Plane Detection mode: Video – thick plate, Video – thin plate
  Video - 4D detection
2 searches – butt joint
  TCH using 1D mode
    Video (ok / NG), multiple searches Video
  EDGE using Gap Measurement mode
    Video; Video;
CIRCLE applications
  Video – moving pipe (outside search)
  Video – moving cut-out (inside search)
  Video – custom macro for changing diameter
  Video – large diameter surface
Applications
  Video – Al welding app
  Video – Coordinated motion
Application Examples

## Slide 17
R*-TCH, 1D mode
Setup
Search Type = 1. touch sensing R1-TCH 1D
When to use AutoTeach modes: 1=small flat surface, 2=larger surface
Exercise: Adjust “AutoTeach Offset” for different plate thickness / surface area

## Slide 18
Setup Section; Overview
Configure settings in “Setup Section” at top of all related macro jobs (Rx-TCH, Rx-EDGE, RxCIRCLE, etc.
  Rapid IN# for AccuFast (TCH, EDGE, CIRCLE)
  Univ Output for AccuFast protective door (TCH, EDGE, CIRCLE)
  AutoTeach Offset (TCH, EDGE)
  Non-search speed (TCH, EDGE, CIRCLE)
  User Frame # (TCH, EDGE, CIRCLE)
  Bvariable # for status (TCH, EDGE, CIRCLE)
  Alarm/no-alarm setting (TCH, EDGE, CIRCLE)
  Retry (if first search missed detection) (TCH, EDGE, CIRCLE)
Set Focal Length for application (if necessary), or use factory configuration
  Set LOW value. Possibly adjust HIGH value if necessary… typically the HIGH value is 10s of mm’s or more from the LOW value which allows for detection using the side of the beam.
Setup

## Slide 19
R*-TCH / R*-EDGE / R*CIRCLE
  Rapid IN# for AccuFast
  Determine which Rapid Input (RIN# / DIN#) is being used by the AccuFast sensor.
  After configuring the Keyence sensor’s LO and HI values, open the shutter door to the sensor and while the red laser dot is projected onto your hand, move your hand between the LO and HI distances.
  You should observe the GO light turns on and, when this does turn on, look at the Rapid Input screen on the PP and determine which RIN# is being triggered.
  Set the Rapid Input # into “SET LI013 (x)”; where x = RIN#
Setup

## Slide 20
R*-TCH / R*-EDGE / R*CIRCLE
  Output door is wired to (Univ Output for AccuFast protective door)
  Consult the system prints of the robot system / Universal Input screen.
  Set the Universal Output # to “SET LI014 (x)”; where x = OT#
Setup

## Slide 21
R*-TCH / R*-EDGE
  AutoTeach Offset (TCH, EDGE)
  With the R*-TCH and R*-EDGE macro jobs, during most AutoTeach motion routines, an “offset distance” is assumed. This distance is adjustable.
  Set desired distance to “SET LI006 (x)”; where x = offset dist.
  Larger value … better accuracy
  Smaller value … use only if flat surface area is small
  Exercise: AutoTeach with TCH and EDGE, adjust parameter
Setup

## Slide 22
R*-TCH / R*-EDGE / R*CIRCLE
  Non-search speed
  The speed used by the macro job routine for motion while searching for surface of the part is adjusted as a Macro Job Argument. The speed used for all other macro job routine motion is set by the “non search speed” parameter.
  Set desired search speed to “SET LI000 (x)”; where x = speed
  User Frame Number
  - If you desire to have the calculated shift amount saved to a User Frame format, you specify the User Frame # here => “SET LB007 (x)”
Setup

## Slide 23
R*-TCH / R*-EDGE / R*CIRCLE
  Bvariable # for status
  At the end of execution of each macro instruction, a value is set to a B variable. The value written to this B variable is either 1 (successful search) or 0 (unsuccessful search). In INFORM you can handle, programmatically, what the robot will do in the event of either situation (success or bad search).
  This parameter allows adjustment of which B variable # the status is written to => SET LB015 (x)
Setup
'--------------------------------
'---- Setup Section ... begin ---
'--------------------------------
MSG ""
'
' Retry on/off
SET LB013 0
'
' Flag status/alarm
' 0=Alarm 1=NoAlarm w/status flag
SET LB014 0
'
' global Bvar address for status
SET LB015 99
SET B[LB015] 0
'
' Manual setting for DX200
' Max shift amount
SET LR000 25
'
*RETRY
'
'LI8 = Robot Number (ie. R1)
SET LI008 1
'
'If using a laser sensor instead
' of touch sense, LI13 = rapid
' input # for laser sensor. Set
' LI13 to 0 if touch sensing is
' used.
SET LI013 0
'
' output laser is wired to
SET LI014 5
'
'LI6 = auto teach offset
SET LI006 10
SET LD000 LI006
'
'LI0 = non search speed
SET LI000 3000
'
'LB7 = userframe number
SET LB007 0
'
'--------------------------------
'-- Setup Section ... complete --
'--------------------------------

## Slide 24
R*-TCH / R*-EDGE / R*CIRCLE
  Flag status/alarm (Alarm/no-alarm setting)
  If a Maximum Shift Amount Exceeded event occurs, an Alarm can be triggered. You can adjust if the alarm is triggered or ignored by the following parameter => “SET LB014 (x) where 0=alarm, 1=no alarm
  Caution!! If ‘no alarm’ is set (SET LB014 1), make sure to collect the value of the Status B Variable and handle (ie. skip a weld job, etc.) in the event of unsuccessful search.
Setup
'--------------------------------
'---- Setup Section ... begin ---
'--------------------------------
MSG ""
'
' Retry on/off
SET LB013 0
'
' Flag status/alarm
' 0=Alarm 1=NoAlarm w/status flag
SET LB014 0
'
' global Bvar address for status
SET LB015 99
SET B[LB015] 0
'
' Manual setting for DX200
' Max shift amount
SET LR000 25
'
*RETRY
'
'LI8 = Robot Number (ie. R1)
SET LI008 1
'
'If using a laser sensor instead
' of touch sense, LI13 = rapid
' input # for laser sensor. Set
' LI13 to 0 if touch sensing is
' used.
SET LI013 0
'
' output laser is wired to
SET LI014 5
'
'LI6 = auto teach offset
SET LI006 10
SET LD000 LI006
'
'LI0 = non search speed
SET LI000 3000
'
'LB7 = userframe number
SET LB007 0
'
'--------------------------------
'-- Setup Section ... complete --
'--------------------------------

## Slide 25
R*-TCH / R*-EDGE / R*CIRCLE
  Retry on/off (if first search missed detection)
  For those applications where occasional missed searches occur, a RETRY of the search motion may be desired. One retry is possible.
  To enable a single Retry => “SET LB013 (x)”; where x=1 (up to two search routines / one retry) or x=0 (one search routine / no retry)
Setup
'--------------------------------
'---- Setup Section ... begin ---
'--------------------------------
MSG ""
'
' Retry on/off
SET LB013 0
'
' Flag status/alarm
' 0=Alarm 1=NoAlarm w/status flag
SET LB014 0
'
' global Bvar address for status
SET LB015 99
SET B[LB015] 0
'
' Manual setting for DX200
' Max shift amount
SET LR000 25
'
*RETRY
'
'LI8 = Robot Number (ie. R1)
SET LI008 1
'
'If using a laser sensor instead
' of touch sense, LI13 = rapid
' input # for laser sensor. Set
' LI13 to 0 if touch sensing is
' used.
SET LI013 0
'
' output laser is wired to
SET LI014 5
'
'LI6 = auto teach offset
SET LI006 10
SET LD000 LI006
'
'LI0 = non search speed
SET LI000 3000
'
'LB7 = userframe number
SET LB007 0
'
'--------------------------------
'-- Setup Section ... complete --
'--------------------------------

## Slide 26
R*-TCH; 2D mode
Programming
TCH macro with 2D mode. touch sensing R1-TCH 2D
  “Robot Positon 1” defines start position for searching motion
  “Robot Positions 2 and 3” define location of Master Part
  Seam Finding technology locates surfaces of deviated part and, comparing to Robot Positions 2 and 3, measures Shift Amount
  Recommended programming sequence:
    1st: Robot Position 2
    2nd: Robot Position 1
    3rd: Robot Position

## Slide 27
R*-TCH; 2D mode
TCH macro with 2D mode
  2touch: AutoTeach
  2touch: Playback
Programming

## Slide 28
R*-TCH; 2D mode
Search Type = 2
Exercise 1: Adjust “Lap Offset” for different plate thickness
Exercise 2: Adjust “AutoTeach Offset” for different lap joint sizes
Setup

## Slide 29
R*-TCH; 2D mode
Search Distance [argument of R*-TCH]: used to define maximum amount of the calculated shift amount, which is based on the distance between “Robot Position 3” and the Detected Location of the seam.
  If the distance between RP3 and the Detected Location is greater than the value of “Search Distance,” the Maximum Shift Amount Exceeded is set. An alarm may be generated, or can be disabled (see value of parameters in SETUP section of macro).
Exercise: adjust and verify that Search Distance can be reduced to tolerate a maximum of +/- 6mm (1/4”) weld seam variation.
Setup

## Slide 30
R*-TCH; 2D mode
Overall search window is defined by:
  Maximum vertical search = (Distance between Robot Position 1 and Robot Position 2) + Search Distance
  Maximum lateral search = (Lateral distance between Robot Position 1 and Robot Position 3) + Search Distance
Exercise 1: move weld seam location until Max Shift Amount Exceeded is set, then adjust Search Distance so the alarm goes away.
Exercise 2: use INFORM to skip a weld if Max Shift Exceeded is set. Use the status flag B variable (referenced in the SETUP section)
Setup

## Slide 31
R*-TCH; 2D mode
Touch Sensing examples: touch sensing R1-TCH 2D w/ weld path
  Flat surface – R1-TCH (1TCH mode)
  T Joint – R1-TCH (2TCH mode).
  6mm Lap – R1-TCH
  2mm Lap, galvanized – R1-TCH
AccuFast examples: accufast R1-TCH
  Edge of thin plate (AutoTeach=1) and Edge of thick plate (AutoTeach=2) – R1-TCH
  Thin Lap – R1-TCH
  Go/no-go, hole in plate – R1-TCH
  Tube-to-tube, using side of laser beam – R1-TCH
Programming; Application

## Slide 32
R*-EDGE
Programming

## Slide 33
R*-EDGE
Programming

## Slide 34
R*-EDGE
EDGE routine
  Mode 0
    Touch sensing
    2D detection
Programming

## Slide 35
R*-EDGE
EDGE routine
  Mode 1
    AccuFast
    2D detection
Programming

## Slide 36
R*-EDGE
EDGE routine
  Mode 2 (Mode 3 = AccuFast)
    Touch sensing
    Gap measurement mode
    2D detection
  Adaptive Welding
    WVADJ instruction
Programming

## Slide 37
R*-EDGE
EDGE routine
  Mode 4 (Mode 5 = AccuFast)
    Touch sensing
    2D w/ Plane-detection mode
Programming

## Slide 38
R*-EDGE
Step Offset [argument of R*-EDGE]:
  Used for Pattern Types 0, 2, and 4
  Defines step size (vertical and horizontal)
  Larger steps = faster cycle time
  Smaller steps = use smaller values if a small gap is to be detected (Pattern Type=2)
Exercise: adjust Step Offset value to detect a 6mm butt joint
Setup

## Slide 39
R*-EDGE
Depth [argument of R*-EDGE]:
  For Pattern Types 0, 2, and 4 …
    Defines distance to move past horizontal surface before moving back to find edge of plate
  For Pattern Types 1, 3, and 5 …
    Defines distance the laser sensor moves into surface before searching for edge of surface
  Larger depth = typically better accuracy for AccuFast
  Smaller depth = use smaller values for thinner plate
Exercise: with AccuFast sensor, adjust Depth value to detect the edge of 6mm sandblasted steel. See how small of a value that can be used before false readings occur
Setup

## Slide 40
R*-EDGE
Search Distance [argument of R*-EDGE]: used to define maximum amount of the calculated shift amount, which is based on the distance between “Robot Position 3” and the Detected Location of the seam.
  If the distance between RP3 and the Detected Location is greater than the value of “Search Distance,” the Maximum Shift Amount Exceeded is set. An alarm may be generated, or can be disabled (see value of parameters in SETUP section of macro).
Exercise: allow for part variation of +/- 6mm. Move the weld seam 8mm and note Maximum Shift Amount Exceeded state.
Setup

## Slide 41
R*-EDGE
Gap Size Output [argument of R*-EDGE]: sets the D variable # that receives the detected Gap amount
Exercise 1: using AccuFast on a 6mm steel butt joint, note the gap distance (placed into a D variable you choose) as the actual gap amount is varied from 2mm to 6mm.
Exercise 2: Call two different Arc Start Files; one if gap is less than 2mm, the other if gap is greater than 2mm.
Setup

## Slide 42
R*-EDGE
Touch Sensing examples: touch sensing R1-EDGE
  Edge, thick plate; Pattern Type 0 – R1-EDGE
  Edge, variable gap on thick plate; Pattern Type 2 – R1-EDGE
  T-joint, oblique angle, variable angle; Pattern Type 4 – R1-EDGE
AccuFast examples: accufast R1-EDGE
  Narrow Butt Joint; Pattern Type 3 – R1-EDGE
  Edge, outside corner; Pattern Type 1 – R1-EDGE
  NSRCH
Programming; Applications

## Slide 43
R*CIRCLE
RxCIRCLE
  3 positions: where RIN turns ON
  3 positions: same Z height (see arguments)
  Circle diameter  D099
  For curved surfaces with ~2” and larger diameters
Programming

## Slide 44
R*CIRCLE
StartSrch Offset [argument of R*CIRCLE]
  Robot Position 1, 2, and 3 represent locations on (location that are touching) the part surface. Approach positions – location used to begin search motion towards Robot Position – are calculated by the macro job…
  This parameter sets the distance between each Robot Position and its approach position
  Exercise: With Touch Sensing, attempt AutoTeach twice, once with “StartSrch Offset” = 5, and again with = 25.
Setup

## Slide 45
R*CIRCLE
Teach Offset [argument of R*CIRCLE]
  During initial teaching of Robot Position 1, 2, and 3, these locations are roughed in by the user. The exact, proper location of these positions are detected by the macro job via AutoTeach.
  The distance between Robot Position 1 and Robot Positions 2/3 – this distance AutoTeach uses – is defined by this parameter.
  Specified in a percentage of the radius of the curved surface. A larger value = better accuracy
  Typical values are in the 25% to 50% range
  Small diameter curved surface => smaller % value
  Larger diameter curved surface => larger % value
  Exercise: Attempt AutoTeach twice, with “Teach Offset” values 10 and 50
Setup

## Slide 46
R*CIRCLE
Max Search Dist. [argument of R*CIRCLE]
  This parameter determines maximum allowable shift amount.
  An alarm can be registered (depending on a SETUP section parameter) when Maximum Shift Amount Exceeded is reached
  Exercise: Adjust parameter to allow +/-6mm part variation. Adjust weld seam 8mm and observe Maximum Shift Amount Exceeded state.
Setup

## Slide 47
R*CIRCLE
out,in,Xin,Xout [argument of R*CIRCLE]
  This parameter determines the search pattern to be used for this instance of R*CIRCLE. Two patterns are available
    0 or 1: 3 point detection. Search pattern as shown in drawing to the right
    2 or 3: 4 point detection. Search pattern with searches at 3, 6, 9, and 12 o’clock.
Exercise: observe all 4 modes
Setup

## Slide 48
R*CIRCLE
Circle Diameter [argument of R*CIRCLE]
  For search patterns of 0 or 1 (‘out,in,Xin,Xout’ = 0 or 1), the macro job makes a calculation to alert the user if a bad search is made.
  To determine if a bad search is made, the diameter of the detected part location is compared to the diameter of the taught part location.
  If the difference in diameter is greater than a threshold value (which is defined in SETUP section), the user is alerted
Setup

## Slide 49
'--------------------------------
'---- Setup Section ... begin ---
'--------------------------------
MSG ""
'
' Retry on/off
SET LB012 0
'
' Flag status/alarm
' 0=Alarm 1=NoAlarm w/status flag
SET LB013 0
'
' global Bvar address for status
SET LB014 99
SET B[LB014] 0
'
*RETRY
'
'LI8 = Robot Number (ie. R1)
SET LI008 1
'
'If using a laser sensor instead
' of touch sense, LI13 = rapid
' input # for laser sensor. Set
' LI13 to 0 if touch sensing is
' used.
SET LI013 0
'
' output laser is wired to
SET LI014 5
'
'LI6 = auto teach offset
SET LI006 10
SET LD000 LI006
'
'LI0 = non search speed
SET LI000 3000
'
'LR4=AllowShiftAmnt as a
' % of Taught circle dia.
SET LR004 10
IFTHENEXP LR004<1 OREXP LR004>20
MSG "Check Allowable Percent Offset"
SETUALM 8001 "R1 INVALID PARAM
PAUSE
ENDIF
DIV LR004 100
'
' Dvar Output for Diameter
' Measurement
SET LB003 99
'
'--------------------------------
R*CIRCLE
Dvar Output for Diameter
  An accurate diameter must be entered into the ‘Circle Diameter’ argument
  Upon successful execution of the R*CIRCLE macro instruction while in AutoTeach mode, the diameter of the taught diameter is written to a D Variable
  The value written into the D Variable should be used for the ‘Circle Diameter’ argument
  This parameter defines which D variable # is used
Exercise: After AutoTeach is complete, collect the measurement of the circle’s diameter from the referenced D variable and input this data to the argument “Circle Diameter”
Setup

## Slide 50
R*CIRCLE
AllowShiftAmnt
  The macro job uses the argument CIRCLE DIAMETER to determine if a bad search (one of the 3 or 4 touches/searches) has been made.
  This parameter sets the allowable difference between the diameter of the detected part location and the diameter of the taught part location.
  Specified in a percentage. i.e. detected diameter=56mm, taught diameter=50, diameter of detected diameter is 12% greater than taught diameter. If AllowShiftAmnt=10, alarm can occur.
Setup
'--------------------------------
'---- Setup Section ... begin ---
'--------------------------------
MSG ""
'
' Retry on/off
SET LB012 0
'
' Flag status/alarm
' 0=Alarm 1=NoAlarm w/status flag
SET LB013 0
'
' global Bvar address for status
SET LB014 99
SET B[LB014] 0
'
*RETRY
'
'LI8 = Robot Number (ie. R1)
SET LI008 1
'
'If using a laser sensor instead
' of touch sense, LI13 = rapid
' input # for laser sensor. Set
' LI13 to 0 if touch sensing is
' used.
SET LI013 0
'
' output laser is wired to
SET LI014 5
'
'LI6 = auto teach offset
SET LI006 10
SET LD000 LI006
'
'LI0 = non search speed
SET LI000 3000
'
'LR4=AllowShiftAmnt as a
' % of Taught circle dia.
SET LR004 10
IFTHENEXP LR004<1 OREXP LR004>20
MSG "Check Allowable Percent Offset"
SETUALM 8001 "R1 INVALID PARAMETERS" 0 SMODE=0
PAUSE
ENDIF
DIV LR004 100
'
' Dvar Output for Diameter
' Measurement
SET LB003 99
'
'--------------------------------

## Slide 51
R*CIRCLE
Touch Sensing example
  Tube-to-plate -- R*CIRCLE
AccuFast example
  Large diameter tube-to-plate -- R*CIRCLE
Programming; Applications

## Slide 52
Path Shifting
Use Macro Instructions to utilize Touch / AccuFast
  R*-TCH, R*-EDGE, R*CIRCLE, etc.
Create/Combine the shift amount(s)
  Use adjacent searches where possible (ie. from other side of plate)
  If 1D variation, search in direction of weld seam movement / variation
  If 2D+ variation, searches must be perpendicular to each other
  Do not compound (ie. X deviation used twice) shift amounts
Deploy SFTON / SFTOF in weld jobs
  R1-TCH P0
  MOVJ
  SFTON P000
  ARCON …
  MOVL
  ARCOF
  SFTOF
Usage

## Slide 53
Path Shifting examples
Combinations
  T-Joint
    one 1D touch on side
    two 2D touches on weld seam (start and end of seam)
Usage

## Slide 54
Path Shifting examples
Combinations
  CRAW coupon
    R1CIRCLE
    one 2D touch at other end
Usage

## Slide 55
Path Shifting examples
Combinations
  Tube-to-tube
    Multiple 1D touches
Usage

## Slide 56
Path Shifting examples
Combinations
  Butt joint
    two EDGE touches on weld seam (start and end of seam)
    WVADJ added to adjust WVON instruction data
Usage

## Slide 57
Overview
Theory in brief
  Requires weaving motion
  Hall Effect sensor  Sensor board  COMARC Inform commands. Regulate welding current with robot path correction.
  Used for steel alloys (not possible with aluminum welding wire)
  MIG welding. Most output modes are supported by Comarc function.
Function information > Comarc Manual
  Equipment Configuration
  Setup / Usage: comarc fundamentals
    Develop seam tracking weld parameters
    Measure PC Data (Comarc Measurement Mode + S1E197=1)
    Measure Comarc settings for weld seam(s) (Comarc Measurement Mode + S1E197=0)
    Deploy settings discovered in step 3. above. Repeat all steps above for different weaving parameter conditions (as needed for your application
Comarc

## Slide 58
Considerations
Required welding conditions:
  Minimize undercut
  High enough travel speed (and low enough wire feed speed) to keep arc at leading edge of weld pool
  Slightly wider weave is more robust than slightly narrower weave motion
  Push angle is better than a drag angle
  Horizonal is better than downhill
  Supported modes: traditional non-pulsed, some (but not all) specialty non-pulsed modes, most pulsed modes. In general, non-adaptive modes are more robust than some adaptive modes.
Comarc

## Slide 59
Tips and pointers
For setup test:
  T-joint 150mm long
  Program weld start location into weld seam
  Deviate weld end point 10-15mm out of the joint (instead of moving the part, move the robot path!)
Comarc

## Slide 60
Tips and pointers
For large variations of weld path:
  Increase parameter SxE30-45 to allow for more aggressive corrections of robot’s path. A larger value produces larger correction amounts for a given amperage change.
For use on butt joints, only U/D correction is possible.
  Reference a Comarc Condition File from the COMARCON instruction. In the C.C. File, set the CORRECTION SELECT setting to “U/D” (instead of U/D & L/R).
Deviation / Correction amount; monitoring
  Use of the C.C. File allows for defining a maximum acceptable distance that Comarc is allowed to deploy. If the actual correction distance is greater than the VERTICAL MONTIOR or HORIZONTAL MONTIOR for the set NO. of times, a robot alarm can be generated based on the CONDITION setting.
U/D adjustment: larger value => shorter CTWD
L/R adjustment: larger value => wire placement is moved to the right
Comarc

## Slide 61
Tips and pointers
Exercise 1: setup for use with Bead-on-Plate welding (ie. use U/D correction only)
Exercise 2: create a T-joint weld sequence with 3 segments. Adjust the L/R value from first segment to last segment to demonstrate control of position of welding electrode (high/low).
Comarc